## Slide 1
Surface:
Au(111) - 9 layers with supercell 2√3 x 3 (1/12 ML, 9 layers, 12 Au atoms)
Au(110) @ 13 layers with supercell surface 3 x 4
A supercell of a gold slab with two water molecules on the surfaces at each side was used to maintain symmetry. Largest slab after Schnur2009.
Kind: Comput.
Details: DFT – SIESTA – GGA (PBE) – DZP basis set – No vdW
Constant electric ﬁeld is used for this work with the direction of the electric ﬁeld oriented normal to the electrode surface with a maximum magnitude of 5 × 109 V/m.
The electrostatic energy suggests that a hydrogen up orientation is energetically more favorable than a ﬂat or a hydrogen down orientation. In the absence of the electric field, the H2O/Au interaction is dominated by Au−O and Au−OH interactions. Water molecules tend to lie virtually parallel to the electrode on atop sites but they lie almost perpendicular to the electrode with hydrogen down on bridge sites without E-field.
Huzayyin2014: Interaction of Water Molecule with Au(111) and Au(110) Surfaces under the Inﬂuence of an External Electric Field

## Slide 2
Surface:
Au(111), Ag(111), Pt(111), Pd / Au(111) and Ru(0001)
4 layers with supercell √3 x √3R30 (Bilayer of water, 7 layers of 16 Au atoms)
Water bilayers on transition metal surfaces
Kind: Comput.
Details: DFT – VASP– GGA (PBE) – PW basis set @ 400 eV
Ice-like hexagonal water bilayers on metal surfaces become strongly polarized which induces a work function reduction at the more strongly interacting transition metal surfaces, irrespective of the orientation of the bilayer. The water bilayers become strongly distorted at room temperature. At the noble metal surfaces Ag(111) and Au(111), the hexagonal water structure is not stable and the water layer becomes disordered. Transitions between H-up and H-down conﬁgurations are well possible and occur frequently so that no distinction between an ordered H-up or an H-down structure can be made.
Charging the metal substrates leads to small but characteristic changes. The change in the
distance from the charged electrodes can be understood invoking electrostatics. The redshift
of the O–H stretch vibrations at the negatively charged electrodes indicates that the addition
of electronic charge to the metal–water interface weakens the intramolecular bonds.
Schnur2009: Properties of metal–water interfaces studied from
ﬁrst principles

## Slide 3
Surface:
Au(111), Ag(111), Pt(111), Pd / Au(111) and Ru(0001)
4 layers with supercell √3 x √3R30 (Bilayer of water, 7 layers of 16 Au atoms)
Au(511) at T = 140 K and T = 300 K
Water layer on stepped Au(511) surface
Kind: Comput.
Details: DFT – VASP– GGA (PBE) – PW basis set @ 500 eV
Structure of water at close-packed metal surfaces is rather liquid- than ice-like.
For Au(511) the oxygen atoms of the water molecules approximately form a ﬂat layer which is only bound through the oxygen atoms above the step atoms. This picture is conﬁrmed by an analysis of the charge density difference upon water adsorption. Thus the water layer is pinned to the metal step atoms whereas the water molecules above the small (100)-like terrace are not directly bound to the metal substrate. This again leads to a stronger water-water interaction which apparently stabilizes the water network. RPBE functional together with semi-empirical dispersion corrections within a RPBE-D approach the wetting behavior of water on close-packed metal surfaces can be correctly reproduced which is not possible using either PBE, PBE-D or pure RPBE calculations. (See tonigold2012)
Gross2014: Water Structures at Metal Electrodes Studied by Ab Initio Molecular Dynamics Simulations

## Slide 4
Surface:
Au(511) Au(100): 15 layers, 4 layers, resp. at T = 140 K and T = 300 K
Water layer on stepped Au(511) and flat Au(100) surface
Kind: Comput.
Details: DFT – VASP– GGA (PBE) – PW basis set @ 400 eV
On Au(100), the rectangular structure obviously dissolves at 140 K. Instead, a more open hydrogen-bonded network of water molecules evolves with almost all water molecules oriented in a plane perpendicular to the (100) surface. At 300 K which is in fact above the desorption temperature of water monolayers from Au surfaces, the resulting structure becomes even more open, reﬂecting the fact that the adsorbed water layer is not thermodynamically stable at room temperature.
The water molecules at the lower step edge are in an H-down conﬁguration. At the lower step edge of the Au(511) surface, we ﬁnd a much larger water monomer adsorption energy of −0.257 eV. Obviously, the water molecules strongly bound to the step edge atoms pin the water structure and lead to a high thermal stability of the water monolayer on Au(511).
Lin2012: First-principles study of the water structure on ﬂat and stepped gold surfaces

## Slide 5
Surface:
Pd(111) and Au(111) 4 layers of 24 Pd (96 in tot) + 80 H2O. Focused on rather Pd.
Two different water sampling. 16 wat at each side of slabs, 80 wat btw two slabs
Pd: 9.715 x 16.826 x 26.968 Å3 / Au: 9.754 x 9.373 x 27.3008 Å3(Table1)
Kind: Comput. !!!
Details: DFT – VASP– GGA (PBE) – PW basis set @ 400 eV. Two vdW treatment. Charged surface.
Structure of water at the interface of these two metals is very different.
Pd111: on average, water molecules from this interface (bottom) are further away from the metal than the molecules on the other interface (top).
Contrary to what has been claimed using classical potentials, the order of water at the interface strongly depends on the metal under consideration and is not always hydrophobic.
For the system with a positive net charge, we observe the formation of the double peak in both interfaces, similar to the previously described ordered domain. On the other hand, when the system has a negative net charge, the number of molecules at both interfaces with down orientations increases, and the disordered domain is formed at the two interfaces. For Au, we do not observe the formation of domains, which is related to the lack of charge transfer at the interface.
Pedroza2015: Local order of liquid water at metallic electrode surfaces

## Slide 6
Kind: Comput. !!!
Details: DFT – CP2K/QS – GPW - GGA (PBE) – GTH pp - DZVP – PW@400 Ry – vdWD3
Three water populations with different conﬁgurations, watA, watB-up and watB-down, were identi ﬁ ed within the interfacial water layer. WatA adsorbs on the metal surface via O atom with its H atoms pointing away from the surface. The adjacent watB-up and
watB-down have one O–H bond parallel to the metal surface, and the other O–H bond points to the liquid water and the metal surface, respectively.
There are clear structural differences between two relatively inert surfaces, namely, Au(111) and Ag(111), and two more reactive surfaces, namely, Pt(111) and Pd(111). Pt(111) and Pd(111) show a higher affinity for watA and watB-down than Au(111) and Ag(111).
Le2017: The structure of metal-water interface at the potential of zero charge fromdensity functional theory-based molecular dynamics
Surface:
Pt-Ag-Pd and Au(111)–water interfaces @330K. 144 Au + 151 H2O molecules, 17.607×17.607×28.188 Å3 for Au.

## Slide 7
Surface:
Pt(111)– and Au(111)–water interfaces. The interface models contain 144 Pt or Au atoms and 151 H2O molecules in total.
16.869 × 16.869 × 27.887 Å3 and 17.607 × 17.607 × 28.188 Å3
Kind: Comput.
Details: DFT – CP2K/QS – GPW - GGA (PBE) – GTH pp - DZVP – PW@400 Ry – vdWD3
The Pt(111) and Au(111)-water interfaces were modelled by fully ﬁlling the vacuum space in the metal surface models with water, and the density of the bulk region is set ∼1 g/mL. The initial conﬁgurations of the surface water were computationally optimised to be H-down ice-like bilayer with 2/3 coverage. The rest of the water molecules were pre-equilibrated with classical molecular dynamics (MD) simulations for ∼100 ps. The conditions of these metal-water interfaces correspond to the potentials of zero charge (PZC). watA, watB and watC, based on their distance to the metal surfaces. Each watA molecule donates 0.05 e- to Au(111) at the PZC. The closest to the surfaces are the watA molecules, mainly sitting on the top site of the metal surfaces (Pt and Au); they are chemisorbed on the surfaces via their oxygen atoms with dipoles (water bisector) pointing outwards, resulting in a partial electron transfer from watA to the metal surfaces.
Le2018: Theoretical insight into the vibrational spectra of metal–water interfaces from density functional theory based molecular dynamics

## Slide 8
Surface:
Au(111)–water interfaces @ 330K with and without inclusion of dispersion correction. 7 layers thick, 12 Au per layer. + 60 H2O. Water layer was equilibrated by classical force ﬁeld. “It would be interesting to see how the recent DFT-D3 and TS methods describe the adsorption structure of water on a gold surface.”
Kind: Comput. !!!
Details: DFT – VASP - GGA (PBE), PBE-D2, optB86b-vdW – PW@300 eV or 500 eV
When the dispersion corrections are included the Au-H2O interaction is stronger. Closest to the surface, H2O is adsorbed O-down, whereas further away it is oriented with one OH bond pointing to the surface and the molecular plane parallel to the normal direction. For the optB86b-vdW functional a third orientation is found where one H atom points into the bulk water layer and the second OH bond is oriented parallel to the metal surface. As for the water density in the ﬁrst adsorption layer we ﬁnd a very small increase of roughly 8%. From the analysis of vibrational spectra a weakening of the H-bond network is observed upon the inclusion of the Au(111) slab,
however, no disruption of H-bonds is observed. While the PBE and PBE-D2 spectra are very similar, the optB86b-vdW spectrum shows that the H-bonds are even more weakened.
Nadler2012: Effect of dispersion correction on the Au(111)-H2O interface: A ﬁrst-principles study

## Slide 9
Surface:
Au(111)–water interfaces @ 400K. 1.5239 nm x 1.4663 nm, 4 atomic layers with 3√3.5 surface. 104 H2O
Kind: Comput. !!!
Details: DFT – CPMD in QE - GGA (PBE), DFT-D – PW@25 Ry
Gold fails to ﬁt theoretical trends, being supposed to behave as a hydrophobic substrate, in terms of interaction energy. On the other hand, most recently, experiments have evidenced that a clean Au(111) surface at room temperature is
hydrophilic. (see Stacchiola2009 for contradiction)
Interaction of a single water molecule with the Au(111) surface at zero temperature: the molecule prefers to adsorb with its oxygen atom at on-top sites with the molecular plane almost parallel to the surface.
The hydrophilicity of a surface is usually related to the ability of a surface to establish hydrogen bonds with water. In the case of Au, it is rather the surface together with its hydration layer that has a hydrophilic character.
Cicero2011: Anomalous Wetting Layer at the Au(111) Surface

## Slide 10
Surface:
Au(111)–water interfaces. The adsorptions of 1 BL, 2 BLs, and 3 BLs of water were each explored.
Kind: Comput & Ex.
Details: DFT –DMol –PW91- 6-31G @ 5 Å cutoff
The results show that gold is, in effect, hydrophobic and that through the formation of intrahydrogen bonding inside of water clusters and as a result of the weak interaction of water with gold, unique double bilayer structures are formed as precursors to the formation of 3D ice clusters.
For 1 BL water adsorption on Au(111), there are two possibilities, having hydrogen atoms pointing up (H-up) or down (H-down). In agreement with previous calculations, our results show that the two structures are very close in energy, with the H-down conﬁguration slightly more stable than the H-up conﬁguration by 0.04 eV/H2O. Overall, our DFT calculations demonstrate that when
increasing the water coverage from 1 BL to 3 BL, the 2 BL structure (H-up|H-down) is energetically favored on Au(111), in agreement with the STM observations/
Investigation presented here support both the original proposal by Smith et al. and later theoretical results that Au(111) is hydrophobic in character. Weak interaction of water with Au that leads to a unique double bilayer formation, which itself is hydrophobic due to the internal locking of hydrogen bonds in the water clusters.
Stacchiola2009 : Water Nucleation on Gold: Existence of a Unique Double Bilayer

## Slide 11
Surface:
Au(111) and Au(001)–water interfaces @ 300K. CMD vs AIMD comparison. 4 layers, Au(001):3 × 3 super cell, 72 gold atoms, Au(111): 4 × 4 super cell, 64 atoms @ 4.88
nm × 4.88 nm and 5.20 nm × 5.20 nm
Kind: Comput.
Details: CMD – DFT – PBE - vdW-DF
For both (111) and (001) surfaces, the lowest energy conformation was a nearly ﬂat water molecule with the oxygen atom on top of a gold atom.
We ran MD simulations of water confined between two gold surfaces for the nine different force ﬁelds. These simulations showed that the force ﬁeld choice has a major effect on the quantitative outcome. By comparing the structural and dynamic properties of water on the Au(111) and Au(001) surfaces, we observed that the water structure is more ordered and dynamics is slower on Au(001) than on Au(111). This distinction is reduced in simulations with softer Buckingham
and Morse potentials compared to LJ simulations. Simulations with ﬁtted Buckingham and Morse potentials were able to yield structural ensembles which are in better agreement with AIMD
results than any of the LJ force ﬁelds.
Berg2017: Evaluation and Optimization of Interface Force Fields for Water on Gold Surfaces

## Slide 12
Surface:
Au(310) : 3-atom wide (100) terraces with monoatomic (110) steps.
Kind: Exp.
Details: -
Falsig et al. have used DFT calculations to investigate CO oxidation on Au(111) and 12-atom Au clusters. They ﬁnd no barrier for the CO+O reaction at the Au(111) terrace. When using Au
clusters, both the adsorption energy and transition state energy for CO+O drop by ~1 eV, thus yielding no signi ﬁ cant activation barrier for CO oxidation at low coordinated Au atoms. Unless the stronger CO–Au bond on Au(310) entirely prohibits CO diffusion below ~160 K and both reactants are fully segregated at the surface, the reaction temperature difference cannot be explained by the variations in adsorption energies and activation barriers. Cited: For Au(111), a single desorption feature appears near 150 K which exhibits zeroth-order desorption kinetics. It was interpreted to indicate formation of 3-dimensional clusters at low coverage and, therefore, that this surface is hydrophobic [12,34]. Water is generally found to initially bind to defects and step edges on other metals that do not dissociate water. A recent DFT study of water adsorption on Au(321), which contains similar 6-fold coordinated Au atoms in the step edge, also ﬁnd these to be the most favorable adsorption sites.
Vanreijzen2011: CO and H2O adsorption and reaction on Au(310)

## Slide 13
Surface:
Au(100), Au(1 11 1), and Au(115): vibration spectrum of H2O (ice) adsorbed at low temperatures
Kind: Exp.
Details: -
On the Au(1 0 0) surface, the spectra show the presence of the typical H-bonded network of water molecules for all coverages from the submonolayer into the multilayer range. The absence of a non-H-bonded OH-stretching mode is indicative for the ‘‘H-down bilayer”. On stepped surfaces, on the other hand, a considerable fraction of the H-atoms remains in the non-H-bonded state; surprisingly even in the multilayer range, and even after annealing. The fraction of non-H-bonded hydrogen atoms scales with the step density.
Spectra of water on stepped gold surfaces show that the bonding of solid water on stepped surfaces differs from Au(1 0 0) and other ﬂat surfaces. A considerable fraction of hydrogen atoms cannot engage in H-bonding, neither in the ﬁrst layer nor in the following layers.
On the other hand, Schnur and Groß have shown very recently that on Au(1 1 1) and Ag(1 1 1) the surface-oxygen distance distribution function of liquid water shows no indication at all for an oxygen-surface bond while such bonds do exist for platinum, palladium and rhodium [8]. The structure of the bilayer is likewise not preserved in liquid water in contact with gold.
Ibach2010: Vibration spectroscopy of water on stepped gold surfaces

## Slide 14
Au(111): Huzayyin2014, Schnur2009, Gross2014, Pedroza2015, Le2018, Nadler2012, Le2017, Stacchiola2009 (comp. & ex.), Berg2017, Friedl2016 (ex.)
Au(110): Huzayyin2014,
Au(100): Lin2012, Berg2017, Ibach2010 (ex.)
Au(511) (stepped): Gross2014, Lin2012,
Au(115): Ibach2010
Au(1 11 1): Ibach2010
Au(310): Vanreijzen2011 (ex.)
Ag-Pt-Pd/Au111-Ru(0001): Schnur2009, Gross2014, Le2017
Pd(111): Pedroza2015
Pt(111): Le2018
Pt(211): Nakamura2009 (One-Dimensional Zigzag Chain of Water Formed on a Stepped Surface)
Pt(533): Kolb2014